Elastic constants.
(Document created by A.R. Oganov, many thanks to D.Vanderbilt and D.R. Hamann).

Elastic constants characterise the ability of a material to deform under any small stresses. They can be described by a fourth-rank tensor Cijkl, relating the second-rank stress tensor ij to the (also second-rank) strain tensor ekl via the generalised Hooke’s law:
ij = Cijklkl , {1}
where multiplication follows the rules of tensor multiplication (see Nye, 1998). Equation {1} can be simplified using the Voigt notation (Nye, 1998), which represents the fourth-rank tensor Cijkl by a square 6*6 matrix Cmn. In these notations, indices ‘11’, ‘22’, ‘33’, ‘12’, ’13’, ‘23’ are represented by only one symbol – 1, 2, 3, 6, 5, and 4, respectively. These notations significantly simplify all equations. So we write instead of {1}:
i = Cijj {2}
Note that infinitesimal strains are being used; in this limit all definitions of strain (e.g., Eulerian, Lagrangian, Hencky, etc.) become equivalent. Under a small strain, the lattice vectors aij’ of the strained crystal is obtained from the old lattice vectors aij0 and the strain tensor eij using the relation:
aij’ = (ij+ij)aij0 . {3}
In the original tensor notation and in the Voigt notation (Nye, 1998), the (ij+eij) matrix is represented as follows:
size 12{ left ( matrix { 1+η rSub { size 8{"11"} } {} # η rSub { size 8{"12"} } {} # η rSub { size 8{"13"} } {} ## η rSub { size 8{"12"} } {} # 1+η rSub { size 8{"22"} } {} # η rSub { size 8{"23"} } {} ## η rSub { size 8{"13"} } {} # η rSub { size 8{"23"} } {} # 1+η rSub { size 8{"33"} } {} } right )} {} = size 12{ left ( matrix { 1+η rSub { size 8{1} } {} # η rSub { size 8{6} } /2 {} # η rSub { size 8{5} } /2 {} ## η rSub { size 8{6} } /2 {} # 1+η rSub { size 8{2} } {} # η rSub { size 8{4} } /2 {} ## η rSub { size 8{5} } /2 {} # η rSub { size 8{4} } /2 {} # 1+η rSub { size 8{3} } {} } right )} {} {4}
The Voigt notation allows one to write elastic constants conveniently as a symmetric 6*6 matrix. Voigt notation is sufficient in most situations; only in rare situations such as a general transformation of the coordinate system the full fourth-rank tensor representation must be used to derive the transformed elastic constants.
One can define the inverse tensor Sijkl (or, in Voigt notations, Sij [1]), often called the elastic compliance tensor:
[1] Note that in Voigt notation Cijkl = Cmn, but Sijkl = Smn only when m and n = 1,2, or 3; when either m or n = 4,5, or 6: 2Sijkl = Smn; when both m and n = 4,5, or 6: 4Sijkl = Smn (Nye, 1998).
{Sijkl} = {Cijkl}-1 or {Sij} = {Cij}-1 {5}
The Sij tensor can be defined via the generalised Hooke’s law in its equivalent formulation:
i = Sijj {6}
There are two groups of experimental methods of measuring the elastic constants: 1) static and low-frequency methods (based on determination of stress-strain relations for static stresses) and 2) high-frequency, or dynamic, methods (e.g., ultrasonic methods, Brillouin spectroscopy, etc.). High-frequency methods generally enable much higher accuracy. Static measurements yield isothermal elastic constants (timescale of the experiment allows thermal equilibrium to be attained within the sample), high-frequency measurements give adiabatic constants (Belikov et al., 1970). The difference, which is entirely due to anharmonic effects (see below), vanishes at 0 K. Adiabatic Cij are larger, usually by a few percent. The following thermodynamic equation gives the difference in terms of thermal pressure tensor bij (Wallace, 1998):
size 12{C rSub { size 8{ ital "ijkl"} } rSup { size 8{S} } =C rSub { size 8{ ital "ijkl"} } rSup { size 8{T} } + { { ital "TV"} over {C rSub { size 8{V} } } } b rSub { size 8{ ital "ij"} } b rSub { size 8{ ital "kl"} } } {} , {7}
where size 12{b rSub { size 8{ ital "ij"} } = \( { { partial σ rSub { size 8{ ital "ij"} } } over { partial T} } \) rSub { size 8{V} } } {} is related to the thermal expansion tensor. For the bulk modulus:
size 12{K rSub { size 8{S} } =K rSub { size 8{T} } \( 1+ ital "αγ"T \) =K rSub { size 8{T} } \( 1+ { {α rSup { size 8{2} } K rSub { size 8{T} } V} over {C rSub { size 8{V} } } } \) } {} {8}
where  and  are the thermal expansion and Grüneisen parameter, respectively.
At constant P,T the elastic constants describing stress-strain relations {1} are given by:
size 12{C rSub { size 8{ ital "ijkl"} } rSup { size 8{T} } = { {1} over {V} } \( { { partial rSup { size 8{2} } G} over { partial η rSub { size 8{ ital "ij"} } partial η rSub { size 8{ ital "kl"} } } } \) rSub { size 8{T} } } {} {9}
while at constant P,S they are given by

size 12{C rSub { size 8{ ital "ijkl"} } rSup { size 8{S} } = { {1} over {V} } \( { { partial rSup { size 8{2} } H} over { partial η rSub { size 8{ ital "ij"} } partial η rSub { size 8{ ital "kl"} } } } \) rSub { size 8{S} } } {} {10}
Now let us derive from {9} an expression for the elastic constants in terms of the second derivatives of the internal energy; in this derivation we follow Ackland and Reed (2003). The unit cell of a crystal can be represented by a matrix size 12{ {V} cSup { size 8{↔} } } {} =(a1,a2,a3), and the volume of the equilibrium unit cell is then size 12{V rSub { size 8{0} } ="det" {V} cSup { size 8{↔} } } {} . Using {4}, for the volume V of a strained cell we obtain:
size 12{ { {V} over {V rSub { size 8{0} } } } = { {"det" {V} cSup { size 8{↔} } } over {"det" {V rSub { size 8{0} } } cSup { size 8{↔} } } } =1+η rSub { size 8{1} } +η rSub { size 8{2} } +η rSub { size 8{3} } +η rSub { size 8{1} } η rSub { size 8{2} } +η rSub { size 8{2} } η rSub { size 8{3} } +η rSub { size 8{1} } η rSub { size 8{3} } - { {η rSub { size 8{4} } rSup { size 8{2} } } over {4} } - { {η rSub { size 8{5} } rSup { size 8{2} } } over {4} } - { {η rSub { size 8{6} } rSup { size 8{2} } } over {4} } +η rSub { size 8{1} } η rSub { size 8{2} } η rSub { size 8{3} } - { {η rSub { size 8{1} } η rSub { size 8{4} } rSup { size 8{2} } } over {4} } - { {η rSub { size 8{2} } η rSub { size 8{5} } rSup { size 8{2} } } over {4} } - { {η rSub { size 8{3} } η rSub { size 8{6} } rSup { size 8{2} } } over {4} } + { {η rSub { size 8{4} } η rSub { size 8{5} } η rSub { size 8{6} } } over {4} } } {} {11}
Then one has in the standard tensor notation:
size 12{ { {ΔV} over {V rSub { size 8{0} } } } =η rSub { size 8{ ital "ii"} } + { {1} over {4} } \( 2δ rSub { size 8{ ital "ij"} } δ rSub { size 8{ ital "kl"} } - δ rSub { size 8{ ital "ik"} } δ rSub { size 8{ ital "jl"} } - δ rSub { size 8{ ital "il"} } δ rSub { size 8{ ital "jk"} } \) η rSub { size 8{ ital "ij"} } η rSub { size 8{ ital "kl"} } +O \( e rSup { size 8{3} } \) } {} {12}
The change of the Gibbs free energy associated with strain is then to the second order:
size 12{ΔG=ΔF+ ital "Pe" rSub { size 8{ ital "ii"} } + { { ital "PV"} over {4} } \( 2δ rSub { size 8{ ital "ij"} } δ rSub { size 8{ ital "kl"} } - δ rSub { size 8{ ital "ik"} } δ rSub { size 8{ ital "jl"} } - δ rSub { size 8{ ital "il"} } δ rSub { size 8{ ital "jk"} } \) η rSub { size 8{ ital "ij"} } η rSub { size 8{ ital "kl"} } } {} {13}
From this one has:
size 12{C rSub { size 8{ ital "ijkl"} } rSup { size 8{T} } = { {1} over {V} } \( { { partial rSup { size 8{2} } F} over { partial η rSub { size 8{ ital "ij"} } partial η rSub { size 8{ ital "kl"} } } } \) rSub { size 8{T} } + { {P} over {2} } \( 2δ rSub { size 8{ ital "ij"} } δ rSub { size 8{ ital "kl"} } - δ rSub { size 8{ ital "il"} } δ rSub { size 8{ ital "jk"} } - δ rSub { size 8{ ital "jl"} } δ rSub { size 8{ ital "ik"} } \) } {} {14a}
and, by analogy,
size 12{C rSub { size 8{ ital "ijkl"} } rSup { size 8{S} } = { {1} over {V} } \( { { partial rSup { size 8{2} } E} over { partial η rSub { size 8{ ital "ij"} } partial η rSub { size 8{ ital "kl"} } } } \) rSub { size 8{S} } + { {P} over {2} } \( 2δ rSub { size 8{ ital "ij"} } δ rSub { size 8{ ital "kl"} } - δ rSub { size 8{ ital "il"} } δ rSub { size 8{ ital "jk"} } - δ rSub { size 8{ ital "jl"} } δ rSub { size 8{ ital "ik"} } \) } {} {14b}
##### It is well known (Barron & Klein, 1965; Wallace, 1998) that under non-zero stresses there can be several different definitions of elastic constants. The constants size 12{B rSub { size 8{ ital "ijkl"} } rSup { size 8{T} } } {} and size 12{B rSub { size 8{ ital "ijkl"} } rSup { size 8{S} } } {} defined by equations {14ab} are those appearing in stress-strain relations and in the conditions of mechanical stability of crystals (see below), whereas the long-wavelength limit of lattice dynamics is controlled by size 12{ { {1} over {V} } \( { { partial rSup { size 8{2} } E} over { partial η rSub { size 8{ ital "ij"} } partial η rSub { size 8{ ital "kl"} } } } \) rSub { size 8{S} } } {} . These two definitions (via stress-strain relations and from long-wavelength lattice dynamics) become idential at zero pressure. Calculating the second derivatives with respect to the finite Lagrangian strains, different equations are obtained (Wallace, 1998).
ABINIT implementation. In ABINIT, the so-called “proper” elastic constants are calculated as follows:
 size 12{C rSub { size 8{ ital "ijkl"} } rSup { size 8{ ital "proper"} } = { {1} over {V rSub { size 8{0} } } } { {d} over {dη rSub { size 8{ ital "kl"} } } } \( Vσ rSub { size 8{ ital "ij"} } \) } {} , {15}
where V0 is the volume of the undeformed crystal at given pressure (stress), and V is the volume changed by strain size 12{η rSub { size 8{ ital "kl"} } } {} . Here we have only the first derivative, so only first-order changes of V are important (to first order, size 12{ { {V} over {V rSub { size 8{0} } } } = { {"det" {V} cSup { size 8{↔} } } over {"det" {V rSub { size 8{0} } } cSup { size 8{↔} } } } =1+η rSub { size 8{1} } +η rSub { size 8{2} } +η rSub { size 8{3} } } {} ). These “proper” elastic constants do not correspond to the stress-strain definition {1}.
size 12{C rSub { size 8{ ital "ijkl"} } rSup { size 8{ ital "proper"} } = { {1} over {V rSub { size 8{0} } } } { {d} over {dη rSub { size 8{ ital "kl"} } } } \( Vσ rSub { size 8{ ital "ij"} } \) = { {1} over {V rSub { size 8{0} } } } { {d} over {dη rSub { size 8{ ital "kl"} } } } \[ V rSub { size 8{0} } \( 1+η rSub { size 8{ ital "kl"} } δ rSub { size 8{ ital "kl"} } \) \( σ rSub { size 8{ ital "ij"} } rSup { size 8{0} } +C rSub { size 8{ ital "ijkl"} } η rSub { size 8{ ital "kl"} } \) \] = { {d} over {dη rSub { size 8{ ital "kl"} } } } \[ σ rSub { size 8{ ital "ij"} } rSup { size 8{0} } +σ rSub { size 8{ ital "ij"} } rSup { size 8{0} } η rSub { size 8{ ital "kl"} } δ rSub { size 8{ ital "kl"} } +O \( η rSup { size 8{2} } \) \] ={}} {}
size 12{ {}=C rSub { size 8{ ital "ijkl"+{}} } { {d} over {dη rSub { size 8{ ital "kl"} } } } \( σ rSub { size 8{ ital "ij"} } rSup { size 8{0} } η rSub { size 8{ ital "kl"} } δ rSub { size 8{ ital "kl"} } \) =C rSub { size 8{ ital "ijkl"} } +σ rSub { size 8{ ital "ij"} } rSup { size 8{0} } δ rSub { size 8{ ital "kl"} } } {} , {16}
where size 12{σ rSub { size 8{ ital "ij"} } rSup { size 8{0} } } {} is the stress in the reference structure (for which the elastic constants are being calculated). From {16} the stress-strain defined elastic constants are:
size 12{C rSub { size 8{ ital "ijkl"} } =C rSub { size 8{ ital "ijkl"} } rSup { size 8{ ital "proper"} } - σ rSub { size 8{ ital "ij"} } rSup { size 8{0} } δ rSub { size 8{ ital "kl"} } } {} {17}
In case of hydrostatic pressure ( size 12{P= - σ rSub { size 8{"11"} } = - σ rSub { size 8{"22"} } = - σ rSub { size 8{"33"} } } {} ) we obtain corrections only for C11, C22, C33, C12, C13, C23, e.g.: size 12{C rSub { size 8{"11"} } =C rSub { size 8{"11"} } rSup { size 8{ ital "proper"} } +P} {} , size 12{C rSub { size 8{"12"} } =C rSub { size 8{"12"} } rSup { size 8{ ital "proper"} } +P} {} .
At non-hydrostatic conditions, the situation becomes more complicated, in particular the Voigt symmetry (Cij=Cji) will be kept only by the “proper” constants – while for stress-strain constants it will be broken, as originally noted by Barron and Klein (1965). For example, from {17} C41 will involve a stress correction, while C14 will not.

REFERENCES:
Barron T.H.K. & Klein M.L. (1965). Second-order elastic constants of a solid under stress. Proc. Phys. Soc. 85, 523-532.
Wallace D.C. (1998). Thermodynamics of Crystals. Dover Publications: N.Y., 484 pp.
Ackland G.J. and Reed S.K. (2003). Two-band second-moment model and an interatomic potential for caesium. Phys. Rev. B67, 174108.